# Materials Science XRD Report: 					XRD2013-0287

| To: | F Miani L Lodya |
| --- | --- |
|  | S Manzini S Potts |
| From: | G Mannsberger |
| Copy: | R Forbes |
| Approved By: | E du Plessis |
| First issued: | 18 November 2013 |
| Updates: |  |
| Pages: | 5 |

XRD ANALYSIS OF IRON AND CARBON BALL MILLED SAMPLES

# Background

Iron and carbon were ball milled for different periods of time . Powder X-ray diffraction analyses were done to determine the crystalline phase present.

# Experimental

The sample name and the assigned sample codes are shown in Table 1.

Table 1 – Sample names

| Sample Name | Sample background | Elements* | BD Number | MC Number |
| --- | --- | --- | --- | --- |
| 1. Fe5C95 BM 4H | Ball milled for 4 hours | Fe, Al, Si, Ag | BD0351 | MC-2013-0734-01 |
| 2. Fe5C95 BM 8H | Ball milled for 8 hours | Fe, Al, Si, Ag | BD0352 | MC-2013-0734-02 |
| 3. Fe5C95 BM 12H | Ball milled for 12 hours | Fe, Si, Ag | BD0353 | MC-2013-0734-03 |
| 4. Fe5C95 BM 16H | Ball milled for 16 hours | Fe, Al, Si, Ag | BD0354 | MC-2013-0734-04 |
| 5. Fe5C95 BM 24H | Ball milled for 24 hours | Fe, Al, Si, Ag | BD0355 | MC-2013-0734-05 |
| 6. Fe5C95 BM 40H | Ball milled for 40 hours | Fe, Al, Si, Ag | BD0356 | MC-2013-0734-06 |

* Elemental analyses from EDX

The samples were packed in PVC sample holders. A Bruker D8 Advance diffractometer was used to carry out the analyses. The data was collected at ambient temperature, atmospheric pressure and the instrument settings were as follows:

Tube voltage			:	40 kV

Tube current			:	40 mA

Source				:	Cobalt (wavelength 1.78897 Å)

Soller slit			:	2.5 °

Fixed divergence slit		:	0.6 mm

Anti-scatter slit			:	2.5 °

Detector			:             Lynx Eye (2.947 °, 0.11 – 0.25V)

Scan from 			:	5 °2

Scan to				:	135 °2

Scan mode                                     :               Locked Coupled

Step size                                         :               0.014324898 °

Time per step                                :               0.1 seconds/step

Scan duration                                :               2 Hours

The crystalline phases present in the samples were identified using X’Pert HighScore Plus©.

# XRD Results

The powder X-ray diffractograms of the ball milled samples are shown in Figure 1 and 2 below:

Figure 1 – X-ray diffractogram of ball milled samples

The sample contains

- Graphite – C

- Iron carbite – Fe2C

- α – Iron – Fe

- Magnetite – Fe3O4

- χ - carbide - χ-Fe5C2

- Θ - Cementite- Θ - Fe3C

Figure 2 – X-ray diffractogram of the Carbon peak

The graphite contribution to the diffractogram was excluded from the Rietveld refinement. The Rietveld refinement results of the remaining crystalline phases are listed in the tables below:

Table 2 Relative abundance (%) of crystalline phases

| Sample Name | α-Fe | Fe2C | Fe3O4 | χ-Fe5C2 | θ-Fe3C |
| --- | --- | --- | --- | --- | --- |
| 1. Fe5C95 BM 4H | 68 | 4 | 1 | 10 | 18 |
| 2. Fe5C95 BM 8H | 73 | 3 | - | 15 | 10 |
| 3. Fe5C95 BM 12H | 63 | - | - | 26 | 10 |
| 4. Fe5C95 BM 16H | 63 | - | - | 29 | 8 |
| 5. Fe5C95 BM 24H | 67 | - | - | 24 | 9 |
| 6. Fe5C95 BM 40H | 62 | - | - | 18 | 20 |

Table 3 Average crystallite size (nm)

| Sample Name | α-Fe | Fe2C | Fe3O4 | χ-Fe5C2 | θ-Fe3C |
| --- | --- | --- | --- | --- | --- |
| 1. Fe5C95 BM 4H | 90(2) | 15(4) | - | 31(7) | 10(1) |
| 2. Fe5C95 BM 8H | 95(3) | 15(6) | - | 23(5) | 10(3) |
| 3. Fe5C95 BM 12H | 102(3) | - | - | 10(1) | 10(2) |
| 4. Fe5C95 BM 16H | 104(3) | - | - | 10(1) | 10(4) |
| 5. Fe5C95 BM 24H | 102(3) | - | - | 10(2) | 10(3) |
| 6. Fe5C95 BM 40H | 86(2) | - | - | 10(2) | 10(1) |

# Comments

It is evident from the diffractogram that the reflections due to graphitic carbon reduced with increasing time of ball milling.